## Slide 1: Extinction and scattering by aggregates composed of submicron particles
Marco Potenza & Llorenç Cremonesi
SCAR AAA 2023
Svalbard, sept 19-21 2023

## Slide 2: AIM of the work
M. A. C. Potenza: Head of the Instrumental Optics Laboratory – University of Milan
We want to characterize dust by measuring light (UV-VIS-NIR-FIR…)
Optical properties of inhomogeneous objects in view of
modelling extinction and radiative transfer processes
L. Cremonesi, et al., Journal of Nanoparticle Research (2020) 22:344 DOI: 10.1007/s11051-020-05075-3

## Slide 3: AIM of the work
We want to characterize dust by measuring light (UV-VIS-NIR-FIR…)
Optical properties of inhomogeneous objects in view of
modelling extinction and radiative transfer processes
Model systems: fractal aggregates
independent characterization
no free parameters
A good model for porous objects, formed by
collision-dominated accretion processes
L. Cremonesi, et al., Journal of Nanoparticle Research (2020) 22:344 DOI: 10.1007/s11051-020-05075-3
M. A. C. Potenza: Head of the Instrumental Optics Laboratory – University of Milan

## Slide 4
The need to describe scattering
by inhomogenous objects
Benisty et al, Optical and Near-infrared View of Planet-forming Disks and Protoplanets, arXiv 2023.09991
M. A. C. Potenza: Head of the Instrumental Optics Laboratory – University of Milan

## Slide 5: Light Scattering was born in Astronomy
M. A. C. Potenza: Head of the Instrumental Optics Laboratory – University of Milan

## Slide 6: Scattering
The incident power is spread
=> scattering cross section
LIGHT
M. A. C. Potenza: Head of the Instrumental Optics Laboratory – University of Milan
Optical particle sizing

## Slide 7: Extinction
The transmitted power is reduced
=> extinction cross section
SENSOR
LIGHT
Scattering
M. A. C. Potenza: Head of the Instrumental Optics Laboratory – University of Milan
Optical particle sizing

## Slide 8: Absorption + = Extinction
SENSOR
LIGHT
Scattering
M. A. C. Potenza: Head of the Instrumental Optics Laboratory – University of Milan
Optical particle sizing (?)

## Slide 9: Optical Particle Sizing ?
«Size» is well defined for objects:
spherical
homogeneous
smooth
amorphous
dielectric
In this case we have a one-to-one relation
between geometrical and optical sizes
Mie Scattering: exact solution of the Maxwell’s Eq.s
M. A. C. Potenza: Head of the Instrumental Optics Laboratory – University of Milan

## Slide 10: Optical Particle Sizing ?
«Size» is well defined for objects:
spherical
homogeneous
smooth
amorphous
dielectric
In this case we have a one-to-one relation
between geometrical and optical sizes
Mie Scattering: exact solution of the Maxwell’s Eq.s
Dust does not have all these properties…
M. A. C. Potenza: Head of the Instrumental Optics Laboratory – University of Milan

## Slide 11
Scattering by inhomogeneous objects
Typically formed by collision-dominated accretion processes
Effective Field Approximation:
Maxwell-Garnett, Bruggemann or other mixing rules:
Maxwell-Garnett
Bruggemann
Others…
M. A. C. Potenza: Head of the Instrumental Optics Laboratory – University of Milan

## Slide 12
Scattering by inhomogeneous objects
Typically formed by collision-dominated accretion processes
Effective Field Approximation:
Maxwell-Garnett, Bruggemann or other mixing rules:
correlations
near field are neglected !
multiple scattering
Average polarization of aggregates => equivalent refractive index
M. A. C. Potenza: Head of the Instrumental Optics Laboratory – University of Milan

## Slide 13
LASER
signal on sensor
Single Particle Extinction and Scattering (SPES)
M. Potenza, T. Sanvito, A. Pullia, AIP Advances 5(2015)117222
M. A. C. Potenza: Head of the Instrumental Optics Laboratory – University of Milan
A self-reference
interference method
No free
parameters
No need for
any calibration

## Slide 14
LASER
signal on sensor
Single Particle Extinction and Scattering (SPES)
A self-reference
interference method
No free
parameters
No need for
any calibration
M. Potenza, T. Sanvito, A. Pullia, AIP Advances 5(2015)117222
M. A. C. Potenza: Head of the Instrumental Optics Laboratory – University of Milan

## Slide 15: Scattering by model inhomogeneous objects
SPES on colloidal
fractal aggregates
Low Angle Scattering:
Size (gyration radius)
Fractal dimension
Re S(0)
Im S(0)
No free parameters
M. A. C. Potenza: Head of the Instrumental Optics Laboratory – University of Milan

## Slide 16: Effective field approximation
Effective field
(Bruggemann)
equivalent sphere
Bruggemann
Re S(0)
Im S(0)
No free parameters
M. A. C. Potenza: Head of the Instrumental Optics Laboratory – University of Milan

## Slide 17
Discrete Dipole
Approximation (DDA)
on model colloidal
fractal aggregates
Bruggemann
Numerical simulations
Re S(0)
Im S(0)
No free parameters
M. A. C. Potenza: Head of the Instrumental Optics Laboratory – University of Milan

## Slide 18
Interpreting the results
Model considering
field-field
correlations
(multiple scattering)
Correlations mainly
affect Re S(0):
The scattered amplitude
is (almost) not affected by correlations
Bruggemann
Re S(0)
Im S(0)
No free parameters
M. A. C. Potenza: Head of the Instrumental Optics Laboratory – University of Milan

## Slide 19
Scattering by
granular spheres
Bruggemann
Interpreting the results
No free parameters
M. A. C. Potenza: Head of the Instrumental Optics Laboratory – University of Milan

## Slide 20
Analytical model
M. A. C. Potenza: Head of the Instrumental Optics Laboratory – University of Milan

## Slide 21
Monomer form factor
Structure factor
Analytical model
M. A. C. Potenza: Head of the Instrumental Optics Laboratory – University of Milan

## Slide 22
Forward scattering by
fractals
(simulations and model)
Bruggemann
Interpreting the results
No free parameters
M. A. C. Potenza: Head of the Instrumental Optics Laboratory – University of Milan
Our model - fractals
Implications for phase functions

## Slide 23
Bruggemann
Interpreting the results
No free parameters
M. A. C. Potenza: Head of the Instrumental Optics Laboratory – University of Milan
Our model - granule
Our model - fractals
Forward scattering by
fractals
(simulations and model)
Implications for phase functions

## Slide 24
Interpretation of the results
No free parameters
M. A. C. Potenza: Head of the Instrumental Optics Laboratory – University of Milan
Bruggemann
Our model
90° scattering by
fractals
(simulations and model)
Implications for phase functions

## Slide 25
Spectral extinction
Models (lines) and
simulations (dots)
N = 500
Rg = 1.6 µm
df = 1.75
No absorption
No n(λ) dependence
No size distr. effects
Bruggemann
Granule
Fractal
No free parameters
M. A. C. Potenza: Head of the Instrumental Optics Laboratory – University of Milan

## Slide 26
Experimental results in the real environment
Simultaneous 0, 45°and 90°scattering
measurements on single airborne particles
OPTAIR @ DomeC
& Ny Alesund
GAIA – Aosta Valley
M. A. C. Potenza: Head of the Instrumental Optics Laboratory – University of Milan
Two populations:
factor 5 in F(90) !!

## Slide 27
Summary
Internal stucture of micron-sized grains influences light scattering and extinction (as expected…)
SPES -> quantitative characterization on model samples
=> validation of the analytical model
M. A. C. Potenza: Head of the Instrumental Optics Laboratory – University of Milan

## Slide 28
Summary
Internal stucture of micron-sized grains influences light scattering and extinction (as expected…)
SPES -> quantitative characterization on model samples
=> validation of the analytical model
Impact on extinction and radiative transfer
single scattering albedo
asymmetry parameter
M. A. C. Potenza: Head of the Instrumental Optics Laboratory – University of Milan

## Slide 29
Summary
Internal stucture of micron-sized grains influences light scattering and extinction (as expected…)
SPES -> quantitative characterization on model samples
=> validation of the analytical model
Impact on extinction and radiative transfer
Atmospheric optics: OPTAIR@Antarctica; paleoclimate studies
Astrophysics: you may figure out… UV-VIS-NIR-FIR…
L. Cremonesi, et al., Light extinction and scattering from aggregates composed of submicron particles, Journal of Nanoparticle Research (2020) 22:344 DOI: 10.1007/s11051-020-05075-3
M. A. C. Potenza: Head of the Instrumental Optics Laboratory – University of Milan

## Slide 30: Thank you Marco Potenza Head Instrumental Optics Laboratory University of Milan marco.potenza@unimi.it